ELECTROPLATING A KEY

Introduction

Electroplating can be used to deposit a layer of metal such as chromium, copper, gold, nickel, or zinc on another metal. This deposit can provide a protective and/or a decorative coating for the metal, which lies beneath it. A common use for electroplating is making faucets for sinks. This laboratory activity will show you how to electroplate a copper coating on a car key or other suitable metallic object.

# Procedure

- Clean the key you are going to plate.  Use vinegar and salt and then rinse with water. Dry the key with a paper towel. Remember your fingers have oils on them and this could interfere with the plating of copper.

- Weigh the key you are going to plate.  Record in data table.

- Fill the beaker ¾ full with electroplating solution.  DO NOT WASTE THIS SOLUTION!

- Make sure your power source is unplugged.

- Clean a piece of copper metal with steel wool.

- Place the copper in the beaker of electroplating solution. Attach the positive wire (the red wire) on the copper.

- Place the key in the solution with the negative wire (the black wire).

- Make sure the copper and the key are not touching.

- Plug the wires into the power source and turn the power source on. Wait for a few minutes.

- Turn off the power, unplug the power source,  and remove the object.

- If you are not satisfied with the plating you can repeat the procedure again.  If it did not work well then you did not clean it good enough.

- Reweigh the key and record in your data table.

Data:

Mass of dry key before process		___________g

Mass of dry key after process		___________g

Amount of copper plated			___________g

Calculations and Questions:

- Why do we need an outside source of electricity for this reaction to occur?

- Which metal is the anode?

Cathode?

- At which electrode does oxidation occur? Reduction?

- Write the half reactions for the substances being oxidized and reduced.

- How many moles of copper were plated on to your key? You must show work!